DIVISION 12 00 00 				FURNISHINGS

SECTION 12 93 00 				SITE FURNISHINGS

SECTION 12 93 23 				TRASH AND LITTER RECEPTORS

BEVEL LITTER RECEPTACLE

Part 1		General

- Summary

  - Section Includes:

    - Litter Receptacle, 22-gallon.

- Submittals

  - Provide submittals in accordance with Section 01 33 00 – Submittal Procedures.

  - Product data:

    - Manufacturer’s standard product literature.

    - Shop drawings.

    - Installation instructions.

    - Maintenance instructions.

  - Submit powdercoat finish samples for approval.

- Quality Assurance

  - Manufacturer Qualifications:

    - Minimum 15 years experience in the manufacture of litter and recycling receptacles.

    - Provide reference list of at least ten major transportation authorities, municipalities, universities, or

other high-use public environments currently using litter and recycling receptacles fabricated by the manufacturer.

- Delivery, Storage and Handling

  - Handle products in accordance with manufacturer’s instructions.

  - Store products in manufacturer’s original packaging until ready for installation.

  - Protect products from impacts and abrasion during storage.

- Warranty

  - Provide manufacturer’s standard warranty:

    - Warranty terms: three years from date of invoice against defects in materials and workmanship.

Part 2		Products

- Manufacturer

  - Basis-of-design product: provide receptacles based on the product named:

1.	Bevel Litter Receptacle by Forms+Surfaces.

2.	Manufacturer Contact:
Forms+Surfaces
30 Pine Street
Pittsburgh, PA 15223
phone: 800-451-0410

fax: 412-385-4715

email: sales@forms-surfaces.com

website: www.forms-surfaces.com

  - Receptacles

    - Materials:

      - Body: TENSL glass fiber reinforced ultra high performance concrete (UHPC).

        - TENSL Material Performance Characteristics:

            - Compressive Strength:  ≥ 18,275 lbs./in² (126 MPa).

            - Flexural Strength:  ≥ 2,756 lbs./in² (19 MPa).

            - Tensile Strength:  1,160 lbs./in² (8 MPa).

            - Water Absorption:  < [measurable limit (kg/m x h0.5)] [3.5%].

      - Liner: black polyethylene with UL94HB fire rating.

      - Door & Back:

        - Stainless steel

        - FSC( 100% Cumaru hardwood slats

      - Hardware: stainless steel.

      - Stainless steel Mounting brackets (sold separately): stainless steel

    - Finishes:

      - Body: intrinsic UHPC finish, Natural color with hydrophobic treatment.

      - Door & back:

        - Stainless steel: polyester powdercoat (Select one option below):

            - Standard Texture from Forms+Surfaces Powdercoat Chart.

            - Custom RAL powdercoat color.

        - FSC( 100% Cumaru hardwood slats: Penofin® hardwood formula “Transparent Natural.”

    - Door & back perforation pattern (for stainless steel door & back only) (Select one option below):

      - None

      - Standard perforation

    - Dimensions and Weight:

      - 25" long x 14" deep x 40" high

      - Stainless steel door & back: 160 lbs. FSC 100% Cumaru door & back: 162 lbs.

    - Mounting:

      - Freestanding.

      - Surface mount. Stainless steel mounting hardware sold separately.

Part 3		Execution

- Examination

  - Verify that substrates are stable and capable of supporting the weight of items covered under this section.

  - Verify that substrates have been adequately prepared to securely anchor those items that will be surface

mounted.

- Installation

  - Install according to the manufacturer’s installation instructions.

  - Install in conformance to applicable ADA guidelines and End User’s established Accessibility policies.

END OF SECTION