DIVISION 12 00 00 				FURNISHINGS

SECTION 12 93 00 				SITE FURNISHINGS

SECTION 12 93 33 				MANUFACTURED PLANTERS

MITER PLANTERS

Part 1		General

- Summary

  - Section Includes:

    - Single 18” high TENSL Ultra High Performance Concrete planter.

    - Double 18” high TENSL Ultra High Performance Concrete planter.

    - Single 30” high TENSL Ultra High Performance Concrete planter.

    - Double 30” high TENSL Ultra High Performance Concrete planter.

- Submittals

  - Provide submittals in accordance with Section 01 33 00 – Submittal Procedures.

  - Product data:

    - Manufacturer’s standard product literature.

    - Shop drawings.

    - Installation instructions.

    - Maintenance instructions.

  - Submit finish samples for approval.

- Quality Assurance

  - Manufacturer Qualifications:

    - Minimum 15 years experience in the manufacture of site seating.

    - Provide reference list of at least ten major transportation authorities, municipalities, universities, or

other high-use public environments currently using site seating fabricated by the manufacturer.

- Delivery, Storage and Handling

  - Handle products in accordance with manufacturer’s instructions.

  - Store products in manufacturer’s original packaging until ready for installation.

  - Protect products from impacts and abrasion during storage.

- Warranty

  - Provide manufacturer’s standard warranty:

    - Warranty terms: three years from date of invoice against defects in materials and workmanship.

Part 2		Products

- Manufacturer

  - Basis-of-design product: provide planters based on the product named:

1.	Miter Planter by Forms+Surfaces.

2.	Manufacturer Contact:
Forms+Surfaces
30 Pine Street
Pittsburgh, PA 15223
phone: 800-451-0410

fax: 412-385-4715

email: sales@forms-surfaces.com

website: www.forms-surfaces.com

  - Planters

    - Materials:

      - Side Panels and Bottom: TENSL glass fiber reinforced ultra high performance concrete (UHPC).

        - TENSL Material Performance Characteristics:

            - Compressive Strength:  ≥ 18,275 lbs./in² (126 MPa).

            - Flexural Strength:  ≥ 2,756 lbs./in² (19 MPa).

            - Tensile Strength:  1,160 lbs./in² (8 MPa).

            - Water Absorption:  < [measurable limit (kg/m x h0.5)] [3.5%].

      - Corner Trim: stainless steel, 4mm thick.

      - Leveling Feet: stainless steel and nylon.

      - Fasteners: stainless steel.

      - Liner: black polyethylene with a UL94HB fire rating.

    - Finish: intrinsic UHPC finish, Natural color with invisible hydrophobic treatment.

    - Dimensions:

      - Single 18” high planter: maximum 3/4” wall thickness, 30” wide x 30” deep x 18.7” high.

      - Double 18” high planter: maximum 3/4” wall thickness, 56” wide x 30” deep x 18.7” high.

      - Single 30” high planter: maximum 3/4” wall thickness, 30” wide x 30” deep x 30.7” high.

      - Double 30” high planter: maximum 3/4” wall thickness, 56” wide x 30” deep x 30.7” high.

    - Mounting:

      - Freestanding.

Part 3		Execution

- Examination

  - Verify that substrates are stable and capable of supporting the weight of items covered under this section.

  - Verify that substrates have been adequately prepared to securely anchor those items that will be surface

mounted.

- Installation

  - Install according to the manufacturer’s installation instructions.

  - Install in conformance to applicable ADA guidelines and End User’s established Accessibility policies.

END OF SECTION