DIVISION 12 00 00 				FURNISHINGS

SECTION 12 93 00 				SITE FURNISHINGS

SECTION 12 93 43 				SITE SEATING AND TABLES

SECTION 12 93 43.13 		SITE SEATING

QUADRA SEATING SYSTEM

Part 1		General

- Summary

  - Section Includes:

    - 17", TENSL UHPC casting with front-to-back aperture, no inset

    - 17", TENSL UHPC casting with Powdercoated aluminum inset

    - 17", TENSL UHPC casting with TENSL UHPC inset

    - 17", TENSL UHPC casting with FSC® Recycled 100% Teak hardwood inset

    - 17", TENSL UHPC casting with planter liner

    - 48", TENSL UHPC casting with front-to-back aperture, no inset

    - 48", TENSL UHPC casting with Powdercoated aluminum inset

    - 48", TENSL UHPC casting with TENSL UHPC inset

    - 48", TENSL UHPC casting with FSC® Recycled 100% Teak hardwood inset

    - 48", TENSL UHPC casting with planter liner

- Submittals

  - Provide submittals in accordance with Section 01 33 00 – Submittal Procedures.

  - Product data:

    - Manufacturer’s standard product literature.

    - Shop drawings.

    - Installation instructions.

    - Maintenance instructions.

  - Submit finish samples for approval.

- Quality Assurance

  - Manufacturer Qualifications:

    - Minimum 15 years experience in the manufacture of site seating.

    - Provide reference list of at least ten major transportation authorities, municipalities, universities, or

other high-use public environments currently using site seating fabricated by the manufacturer.

- Delivery, Storage and Handling

  - Handle products in accordance with manufacturer’s instructions.

  - Store products in manufacturer’s original packaging until ready for installation.

  - Protect products from impacts and abrasion during storage.

- Warranty

  - Provide manufacturer’s standard warranty:

    - Warranty terms: three years from date of invoice against defects in materials and workmanship.

Part 2		Products

- Manufacturer

  - Basis-of-design product: provide seating system modules based on the product named:

1.	Quadra Seating System by Forms+Surfaces.

2.	Manufacturer Contact:
Forms+Surfaces
30 Pine Street
Pittsburgh, PA 15223
phone: 800-451-0410

fax: 412-385-4715

email: sales@forms-surfaces.com

website: www.forms-surfaces.com

  - Module

    - Material:

      - Body: cast TENSL glass fiber reinforced ultra high-performance concrete (UHPC).

        - TENSL Material Performance Characteristics:

            - Compressive Strength:  ≥ 18,275 lbs./in² (126 MPa).

            - Flexural Strength:  ≥ 2,756 lbs./in² (19 MPa).

            - Tensile Strength:  1,160 lbs./in² (8 MPa).

            - Water Absorption:  < [measurable limit (kg/m x h0.5)] [3.5%].

      - Base: cast aluminum.

    - Finishes:

      - Body: intrinsic UHPC finish, Natural color with hydrophobic treatment.

      - Base: cast aluminum in Slate Texture Powdercoat.

    - Dimensions and Weight:

      - Overall dimensions and Weight:

        - TENSL UHPC casting with front-to-back aperture, no inset: 17" long x 17" deep x 17.8" high, 164 lbs.

        - TENSL UHPC casting with aluminum inset: 17" long x 17" deep x 17.8" high, 180 lbs.

        - TENSL UHPC casting with TENSL UHPC inset: 17" long x 17" deep x 17.8" high. 192 lbs.

        - TENSL UHPC casting with hardwood inset: 17" long x 17" deep x 17.8" high. 180 lbs.

        - TENSL UHPC casting with planter liner: 17" long x 17" deep x 17.8" high. 177 lbs.

        - TENSL UHPC casting with front-to-back aperture, no inset: 48.8" long x 17" deep x 17.9" high, 340 lbs.

        - TENSL UHPC casting with aluminum inset: 48.8" long x 17" deep x 17.9" high, 379 lbs.

        - TENSL UHPC casting with TENSL UHPC inset: 48.8" long x 17" deep x 17.9" high. 416 lbs.

        - TENSL UHPC casting with hardwood inset: 48.8" long x 17" deep x 17.9" high. 379 lbs.

        - TENSL UHPC casting with planter liner: 48.8" long x 17" deep x 17.9" high. 369 lbs.

    - Mounting:

      - Freestanding.

      - Surface mount. Stainless steel anchors and mounting bolts are sold separately.

  - Inset

    - Material (Select one option below):

      - Aluminum.

      - TENSL UHPC (Select one option below):

        - No pattern.

        - Bias pattern.

      - FSC® Recycled 100% Teak hardwood.

      - Planter liner: black polyethylene with UL94HB fire-rating.

      - Aluminum with planter liner.

      - TENSL UHPC with planter liner: black polyethylene with UL94HB fire-rating (Select one option below):

        - No pattern.

        - Bias pattern.

      - FSC®  Recycled 100% Teak hardwood with planter liner.

    - Finishes:

      - Aluminum inset (if selected, choose one option below):

        - Standard Texture from Forms+Surfaces Powdercoat Chart.

        - Custom RAL Powdercoat color.

      - Module: intrinsic UHPC finish, Natural color with hydrophobic treatment.

      - Hardwood slats: Penofin® hardwood formula “Transparent Natural.”

Part 3		Execution

- Examination

  - Verify that substrates are stable and capable of supporting the weight of items covered under this section.

  - Verify that substrates have been adequately prepared to securely anchor those items that will be surface

mounted.

- Installation

  - Install according to the manufacturer’s installation instructions.

  - Install in conformance to applicable ADA guidelines and End User’s established Accessibility policies.

END OF SECTION